P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55 /General conditions and A90 & A94.

PRODUCTS

310A	 AIR TIGHT & HUMIDITY-VARIABLE VAPOUR CHECK MEMBRANE:

System: Complete intelligent air-tightness system with all necessary adhesive agents.

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Reference: Pro clima Intello Plus

Accreditation:

CE Mark in accordance with DIN EN 13984

NSAI Agrément Certificate: NSAI 07/0297

Importing Agents: Ecological Building Systems See P14/509K

UK & Ireland Agent: Ecological Building Systems UK Ltd. See P14/509K

Product Page: http://www.greenspec.co.uk/html/product-pages/intello_plus.php

Properties: Airtight and vapour permeable, easy to apply, no splicing or tear propagation due to reinforcing layer.

Breaking Load:

MD: 425 N/50mm.

CD: 280 N/50mm.

Durability: to EN 13984

Application:

Internal face only

Roofs, walls & floors

Difficult to protect against condensation: Flat roofs, flexible metal sheeting

Fire Rating E

Material: 100 % polyolefins,

Membrane: Polyethylene copolymer

Fleece: Polypropylene

Reinforcement layer: Polypropylene

Manufacture: assembled by extrusion coating process involving heat and pressure.

Colour: Translucent, white with black and green text or markings

These materials allow for easy recycling.

Water Vapour Transmission Resistance:

sd: <0.25 m to >10.5 m (humidity variable)

Permeance : >13.2 to <0.33 US perms

MVTR: humidity-variable range: <1.28 to >51 MNs/g

Temperature resistance: -40 to +80 degrees C

Diffusion resistance factor: 37.500

Standard dew point assessment/calculation to BS EN 13788

Thickness: 0.2 mm.

Surface weight: 125 g/m2.

Roll size: 1500 mm. x 20 or 50 m. (standard sizes, others available subject to order, upon request)

Environmental Credentials:

Country of origin and manufacture: Germany,

Attributes:

Diffusion Open product for use in breathing construction,

Use with the following sealing adhesive tapes and adhesives:

Adhesives: Orcon F to P14/322A

Adhesive tapes:

Unitape to P14/330A

Tescon No. 1 to P14/336A

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/