P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55/General Conditions and A90 & A94.

PRODUCTS

336A	 CORNER AIRTIGHTNESS SEALING ADHESIVE TAPE:

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Product Reference: Tescon Profil

Importing Agents: Ecological Building Systems See P14/509K

Product Page: http://www.greenspec.co.uk/html/product-pages/tescon_profile.php

3rd party accreditation:

NSAI Agrément Certificate: NSAI 07/0297

Type: Single sided, flexible, multi-purpose adhesive tape with 3-part release paper

Application:

Internal and external

for quick and awkward tight corners at perimeter of windows doors and rooflights

Colour: dark blue

Size: 60 mm. wide x 30 m.

Properties:

Tears off easily by hand

High flexibility

High elasticity: resistant to piercing in corners

Release papers separate easily

Life expectancy: 60+ years

Temperature resistance: -40 to +90 degrees C

Airtight bonding to DIN 4108-7, SIA 180 and ONorm B8110-2

Materials:

Backing: perforated Polyethylene PE-foil and adhesive

Acrylate which is free from solvents and softeners

Use with:

Pro clima Intello Plus to P14/310A

Pro clima DB+ to P14/311A

Pro clima Solitex Plus to P14/317A

Application:

Internal and external corner joints, sealing reveals,

Abutments with windows,

Abutments with roof windows,

Abutments with doors,

Abutments with planed timber.

It is equipped with three strips of release paper.

This allows ‘activation’ of a single part of the adhesive surface and sealing of one side at a time.

In the second step, remove the remainder of the release paper and finish the sealing of the joint.

Tools: Pressure applicator: to P14/390A

Delay between taping/sealing and air testing: Generally: 10 minutes minimum.

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/