P14	AIR/WIND TIGHTNESS VAPOUR PERMEABLE LAYERS

To be read with the Preliminaries A10-A55 /General Conditions and A90 & A94.

PRODUCTS

314B	AIR TIGHT VAPOUR CHECK VAPOUR CHECK SEALING STRIP:

System: vapour check air-tightness sealing strip with all necessary adhesive agents.

Manufacturer: MOLL bauökologische Produkte GmbH, See P14/509K

Reference: Pro clima DA-S

Accreditation:

CE Mark in accordance with DIN EN 13984

IAB Certificate 07/0297 Pro clima intelligent airtight system

Importing Agents: Ecological Building Systems See P14/509K

Backgrounds: Plywood, chipboard, OSB, concrete, timber, membranes,

Applications:

Internal only

Airtight sealing strip at critical junctions between building materials:

(e.g. OSB to concrete) in accordance to DIN 4108,

For roof, roof slopes, walls and floors,

Eaves and gables,

Skirting junction with floor

Large gaps at junctions to windows and doors

Materials with short term moisture penetration

Properties:

Weatherproof, water repellent and water resistant

Air tight sealing layer and generally applied on the inside of insulation

Fire Rating E

Material: made up of two layers

Robust polypropylene protection fleece, Halogen free polypropylene film

Temperature resistance: -40 degrees C to +90 degrees C

Life expectancy: 60 years +

Roll size: 210 mm. x 100 m.

Environmental Credentials:

Country of origin and manufacture: Germany,

Attributes:

Vapour check and airtight,

Site issues:

Protects the building from the weather during construction

Protecting structure during construction phase

More resistant to site conditions than other vapour checks

Can be exposed to the elements for 4 months.

When applied externally it is not possible to perform quality control testing either using a pressure differential method such as using the Pro clima Wincon see P14/690 or by means of a visual test, such as the Blower Door See P14/910 & 970

It is therefore imperative that all taping and attachment is done with utmost care.

Ensure detailed planning, particularly of fitting at the eaves and gables,

Ensure careful execution when fitting insulation over rafters.

Use with:

Adhesives: Pro clima Orcon F: to P14/322A,

Adhesive tapes: Tescon No. 1 to P14/332A,

Tools: Double dispensing gun: to P14/392A.

Delay between taping/sealing and air testing: Generally: 10 minutes minimum.

© 2000-2009 NGS GreenSpec

REV	REVISIONS

| Revision No | Description | Author | Date | Checked by |
| --- | --- | --- | --- | --- |
| A00 | For Preliminary Issue Extracted from Specification file A11 %%% | BRM | 14/12/2009 |  |
| B00 | Reviewed, post on Website |  |  |  |

Terms and Conditions

1 The ‘Information’

1.1 The ‘Green Building Specification’ is a service provided by GreenSpec.  These terms and conditions may be revised from time to time without prior notice.

1.2 This draft specification was prepared for the GreenSpec ‘Green Building Specification’ by Architectural Specification Writing Services (ASWS).

1.3 The specification clauses in this document (the 'Information') are based on past project work, information gathered from seminars, workshops and assimilated from published or unpublished verbal and written information.

1.4 The Information will continue to be developed and current files will be maintained on the GreenSpec website at www.greenspec.co.uk

2 Copyright Notice

2.1 Copyright and all other intellectual property rights in the Information shall remain at all times the property of GreenSpec and you shall acquire no rights in any such material except as expressly provided in this Agreement.

2.2 You are permitted to reproduce any part or parts either alone or in conjunction with your own material for the purposes of internal use in the your office, or for inclusion in any drawings or contract documents used or intended to be used in connection with a building contract where you are contracting party, or in connection with which you are engaged by one of the contracting parties in a professional capacity.

2.3 You shall not use, sell, assign, rent, sub-license, loan, or otherwise deal in any way in the Information or any interest in it except as expressly provided herein.

3 Disclaimer

3.1 Whilst GreenSpec endeavours to ensure that the Information is correct, it is provided on an "as is" basis, without warranties of any kind, and no warranty, express or implied, is given as to accuracy, currency or completeness and GreenSpec does not accept any liability for any error or omission.  GreenSpec shall not be liable for any third party claims or losses of any nature including, but not limited to, loss of profits, direct, indirect, special or consequential damages arising from a third party's use or inability to use this Information.

3.2 All users and others must verify the contents of the Information and ensure that its application is effective to communicate what is required by them and that the Information is fit for their intended use which has not been specified by GreenSpec.

3.3 GreenSpec accepts no responsibility for the content on any internet website to which a hypertext link from this specification exists.  The links are provided "as is" with no warranty, express or implied, for the information provided within them.

4 General

4.1 If any part of this Agreement is held by a court of competent jurisdiction to be unenforceable the validity of the remainder of the Agreement will not be affected.

4.2 This Agreement is covered by the Laws of England and Wales.

______________________________________________________]

Addenda

NBS compatibility

National Building Specification (NBS) is the industry standard specification library.

GreenSpec’s Green Building Specification (GBS) is designed to complement NBS.

GreenSpec clauses are written specifically to address issues of environmental sustainability.

NBS adopts and develops the Construction Project Information Committee’s (CPIC) classification system Common Arrangement of Work Sections (CAWS) 1998 edition.

GBS adopts and develops the CPIC and NBS versions of CAWS to enable integration into NBS-based specifications.

GBS adopts NBS clause numbering to provide for easy clause assimilation.

CPIC: www.productioninformation.org/

CAWS: www.productioninformation.org/CAWS.asp

Proposed changes: www.productioninformation.org/cawsuni/topcawsuni.asp

NBS: www.thenbs.com/